## Slide 1
Specifications | V6450
Capacity | 50Ah
Nominal Voltage | 64 Volts
Full Charge Resting Voltage | 70 Volts
Energy Storage | 3200Wh (3.2KWh)
Run time @ 100 Amp load | 0.5Hours @ 77°F (25℃)
Self Discharge Rate | ≤4%/Month
Charging | 
Charging Temperate Range | 32~131°F
Charge Method | CC/CV
Maximum Current | 50Amps @ 77°F (25℃)
Recommended Current | 25Amps
Charge Efficiency | 99%
Discharging | 
Discharging Temperate Range | -4~140°F
Discharge Current | 50Amps Continuous
Discharge Current 3 seconds | 200Amps
Discharge Cut-off Voltage | 50Volts; Any cell (2.5 Volts)
Recommended Low Voltage Disconnect | 50Volts
Short Circuit Protection | 400A for 900µS
Short Circuit Protection Release | Disconnect the load
Battery Protection | 
Over Voltage, per Cell, Open | 3.65 Volts ± 0.03 Volts
Over Voltage, per Cell, Release | 3.40Volts ± 0.05 Volts
Over Discharge, per Cell, Open | 2.5 Volts ± 0.05 Volts
Over Discharge, per Cell, Release | 2.7 Volts ± 0.05 Volts
Over Current | 70Amps 32S
Over Current Release | Disconnect the charger or load
Over Temperature | 140°F (60℃)
Over Temperature Release | 122°F (50℃)
Low Temperature Charge, Open | 35.6°F
Low Temperature Charge, Release | 41°F
MOSFET Over Temperature, Open | 194°F
MOSFET Over Temperature, Release | 158°F
Mechanical | 
Length | 19.33’’（491mm）
Width | 12.44’’ (316mm)
Height | 7.83’’ (199mm)
Weight | 72.7 Pounds (33Kg)
Hardware | M8 Bolts, Washer, Lock Washer
Hardware Torque | 88 in - lb. (9 N-m)
Miscellaneous | 
Discharge Test | 100% DoD @ 1C
Discharge Test Results | ＞3000 cycles ~ 80% remaining Capactiy
Storage Method | 50% SoC, test @ 90 Days, recharge if below 43.2V
Storage Temperature Range(Recommended) | -4°F ~ 95°F (-20℃ - 35℃)
Lithium ion Chemistry | Lithium Iron Phosphate (LiFePo4)
Internal Impedance(50% SoC) | ＜ 25mΩ